## Slide 1: Cryogenic Integration In Modern Materials Manufacturing
Cryogenic Mechanical Systems Development For Polymer-Based Raw Materials Manufacturing
Fernando Velez (R&D Mechanical Engineer)

## Slide 2: Table of Contents
2
  Cryogenic Ball Milling of Metallic Materials
  Cryogenic Integration In Polymer Materials
  Mechanical Engineering Methodology
  Achieving Cryogenic Temperatures
  Cryo-Burr Mill Temperature Achievements
  Polymer Particle Reduction Analysis
  Manufacturing Financial Overview
  Future Cryo-Burr Initiatives

## Slide 3: Cryogenic Ball Milling of Metallic Materials
Metallic Powder Morphology Illustration
As received
(Spherical GA powder)
Flattening
High Aspect Ratio Flake
Cryogenic Material Processing
Cal Nano advances cryogenic metal milling technologies to industrial grinding for commercial production of polymer-based materials
New R&D engineering efforts in industrial machinery, cryogenic line retrofitting, and particle size reduction methods
New customers, material processing demand, operating procedures, safety standards, and infrastructure
Agglomeration
Cryo-milling: Material embrittlement through low temperature environments. High energy impact reduces the particle sizes of various materials into extremely finer powders

## Slide 4: Cryogenic Integration In Polymer Materials
4
Strategic R&D investments in polymer-based raw-materials manufacturing prototypes
Gaseous nitrogen replaces cryo-liquids for industrial grinding of polymer materials
Polymer-based materials operate at distinct glass transition temperatures
Prototype technology requires new engineering design and experimental testing
Mechanical systems offers greater control in polymer particle size reductions
Ambient Conditions
, ,
Nitrogen Inlet
Experimental Material Inflow
C.S.
Control System
, ,
Cryogenic Material Outflow
Energy System Input
Heat Transfer
Heat Generation

## Slide 5: Mechanical Engineering Methodology
Considerations:
Optimal Material Temperatures/Pressures
Applicable Nitrogen Phase-States
Ideal/Non-Ideal Conditions in System
Control Volume Analysis of Combined Properties
Gaseous Nitrogen Mass Flow Rates
Considerations:
Hybrid Machine Performance
Natural/Forced Flow
Maximum Feed Rates
Heat Development
Material Heat Mitigation
Nitrogen Material Testing
Prototyping & Experimentation
Harsh Environmental Factors
Nitrogen Material Reactivity
Considerations:
Analysis of Experimental Data
Particle Size Sample Testing
Cryogenic Sampling & Quality Testing
Material Glass Transition Temperatures
Experimental Data Collection
Thermocouples, Pressure Sensors, Flow Meters, Etc.
Data Acquisition in Harsh Environments
Step 1: Material Reactivity
Step 2: Nitrogen Retrofitting
Step 3 Cryogenic Material Processing
Desired Material?
No
Yes
Computational Analysis
CAD, FEA, CFD, Etc.
Accurate?
Iterative Optimization
Subcomponent Redesign, Nitrogen Phase-State Adjustments, Thermodynamic Calculations, Etc.
Industrialize Process
Source Applicable Equipment, Develop Supply Chains, Scale Production, Standardize Procedures, Etc.

## Slide 6: Cryo-Burr Mill Temperature Achievements
Chart: Synthetic Polymer Material Processing
| 1 | 30 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300 | 330 | 360 | 390 | 420 | 450 | 480 | 510 | 540 | 570 | 600 | 630 | 660 | 690 | 720 | 750 | 780 | 810 | 840 | 870 | 900 | 930 | 960 | 990 | 1020
Experiment 1 | 21.2 | 23.7 | 28.2 | 31.4 | 34.7 | 36.4 | 39.5 | 40.6 | 43.4 | 44.1 | 47.6 | 47.8 | 50.7 | 50.3 | 54 | 53.5 | 56 | 56.1 | 58.3 | 57.1 | 59.8 | 58.6 | 60.7 | 59.7 | 62 | 60.5 | 62.9 | 61.8 | 63.7 | 62 | 64.6 | 62.9 | 65.5 | 62.1 | 64.7
Experiment 2 | 19.8 | 22.4 | 24.8 | 27.2 | 30 | 34 | 35.9 | 37.5 | 41.5 | 36.6 | 36.6 | 45 | 46.9 | 47.2 | 42 | 40.9 | 44.8 | 45.4 | 45.5 | 44.9 | 48.6 | 46.7 | 47.7 | 46.3 | 47.2 | 46 | 48.1 | 55.9 | 60.9 | 53.7 | 60.2 | 54.4 | 71.8 | 59.4 | 70.8

## Slide 7: Polymer Particle Reduction Analysis
Chart: PSA Material Sampling Data
| Sample 1 (710μm Particles) | Sample 2 (630μm Particles) | Sample 3 (490μm Particles)
Test 1 | 718.5 | 672.1 | 544.5
Test 2 | 713 | 658.2 | 583.5
Test 3 | 761.1 | 676.4 | 564.8

## Slide 8: Manufacturing Financial Overview
8
Cryogenic mechanical hybrid systems resulted in large-scale production success at lower costs and personnel
Cryogenic material processing technology allowed for further particle reductions in polymer-based materials and an increase in material production
New customer orders from AbTech Industries Inc. resulted in company technology investments, rapid market entry, and greater product demand
Thermodynamic Diagram
Quarter | Particle Reduction (μm) | Production Growth (lb./day) | Customer Demand
Q1 | ~710 | ~50 | 1,000 lb. / month
Q2 | ~490 | ~410 | 4,000 lb. / bi-weekly

## Slide 9: Future Cryo-Burr Initiatives
Increase robustness of cryogenic hybrid systems
Integrate further safety standards & operations
Identify new opportunities and industry sectors
Scale infrastructure & material quality
Expand growth trends through new materials
9

## Slide 10: Fernando Velez
Location: Los Angeles, CA 90063
Phone: +1 (323) 852-2014
Email: fernvel36@gmail.com
LinkedIn: https://www.linkedin.com/in/fernando-velez-679118192
R&D Mechanical Engineer
10

## Slide 11: References
California Nanotechnologies Advances Commercial Production with Two Purchase Orders and ISO 9001 Certification. (Apr 21, 2025). https://www.calnanocorp.com/california-nanotechnologies-advances-commercial-production-with-two-purchase-orders-and-iso-9001-certification
California Nanotechnologies Presentation. (2023, March). https://www.calnanocorp.com/Cal-Nano-Presentation-March-2023.pdf